## Slide 1: Mechanically Testing Bone Tissue
Snehal Shetye, Rob Mauck

## Slide 2: Function of the Skeleton
Support and protection for internal organs
Attachment sites for muscles allowing movement of limbs
Structure support for bone marrow and blood vessels
Mineral reservoir for calcium and phosphorus
Endocrine organ
  Osteocalcin
  FGF23

## Slide 3: Adaptation to Load
G.H. von Meyer’s trabecular bone architecture in human femur (1867)
Principal stress trajectories of Culmann’s crane and human femur (1870)

## Slide 4: Tension/Compression Test
Bone material property (mesoscale)
Test region
Extensometer arms firmly attached with rubber bands
Bone ends embedded in metal end caps
Testing machine slowly applies force to specimen
Force
Deformation

## Slide 5: Compression test
Bone material property (microscale)
  Bone micropillar manufactured by focused ion beam
  Uniaxial compression
  Stress-Strain curve
Stress
Strain

## Slide 6: Nanoindentation
Bone material property (nanoscale)
Birkovich tip

## Slide 7: Load Response of Bone
Cortical bone

## Slide 8: Load Response of Bone
Trabecular bone

## Slide 9: In Vivo loading of bone
Ulnar overloading
Non-invasive ACL rupture
Tibial overloading

## Slide 10: 3-point Bending
3-point test
Load (F)

## Slide 11: Shear and Moment Diagram
Maximum moment at center point of beam

## Slide 12: 4-point Bending
4-point test
Load

## Slide 13: Shear and Moment Diagram
Maximum moment spans distance between top actuators

## Slide 14: Parameters
Maximum Flexural Stress
    Here, is 2nd moment of inertia, = moment applied at middle of specimen, = distance from center of specimen to convex surface
Elastic Modulus
  (for 3-point bending)
  (for 4-point bending)
    Here, is deflection at max. force, is length between bottom supports, and is max. force
Bending Stiffness
  Slope of linear region from force-displacement curve
Tension
Compression

## Slide 15: How do we calculate ?
Laws of static mechanics:
  Sum of all forces
  Sum of all moments at a single point
    These two equations will resolve the unknown reaction forces at the bottom supports
    Moment at any point can now be calculated
3-point Bending:
4-point Bending

## Slide 16: How do we calculate ?
This is difficult for biological specimens
For bone
  Obtain uCT scans of mid-shaft
  We have a custom MATLAB code that calculates for any chosen axis (Bending Buddy)
  This code also estimates by fitting circle to bone cross-section and obtaining equivalent radius

## Slide 17: Stuff to Consider
Measure length of all your samples to determine proper support spacing
3-point bending not recommended for fractured bone
4-point bending is generally always recommended over 3-point unless tissue is too small
Torsion tests work well for fractured specimens
Most ideal to test all samples on same day (day-to-day variation in test setup can influence results)
Keep orientation constant for all samples!
  Find a stable orientation such that bone does not rotate while being loaded

## Slide 18: Example
4-point bend setup

## Slide 19: Failure modes in bone

## Slide 20: When to use torsion tests?
3-pt or 4-pt bend tests work well for intact specimens
Fractured samples
  3-pt test will cause significant stress concentrations at the contact point
    Usually that is where the fracture/callus is
    Definitely not recommended
  4-pt test loading points should span the healing site
    Difficult to achieve on mouse femora/tibiae
    Cannot control size and location of fracture callus
  Torsion
    Usually have unobstructed access to epiphysis
    Only test that evaluates the entire free length of the bone
    Does need 6-dof fixation at the termini
    Takes longer for prep and setup
Load (F)
Load

## Slide 21: Torsion testing

## Slide 22: Torsion Parameters
Polar Moment of Inertia
  - perpendicular axis theorem
  Obtain and from Bending Buddy
    Requires uCT scan for each sample
  Don’t use default output from uCT

## Slide 23: Polar moment of inertia
Shear modulus
  Parameters we can report
    Max. torque
    Angular rotation at max. torque
    Torsional stiffness
    Shear Modulus ()
    Torsional Rigidity ()
    Where is max. torque applied, is length of specimen being tested, and is twist (in radians) at max. torque
Things to remember
  Expect a spiral fracture
  Make sure to take a gauge length image to obtain
    And a scale image!
  If testing fractured samples, each sample needs to be mostly straight and vertical

## Slide 24: Torsion Testing