## Slide 1: Mechanical Response of Tendons, Ligaments, and Skin: A Practical Approach
Snehal Shetye, Ph.D.
PCMD Biomechanics Core
Learning Lunch – June 14th, 2019

## Slide 2: Feedback
People want to review a lot of theory related to:
  Deformation of a body
  Infinitesimal and finite strain theory
  Deformation tensors
  Continuum mechanical theory

## Slide 3: Let’s get into it.

## Slide 4: Just kidding…

## Slide 5: Tendon/Ligament
Tendon Mechanics
  The fundamental function of a tendon is to transfer load
    How does this happen?
    How do we quantify it?
Tendon Structure
  Hierarchical -> How to quantify?
    Realignment
    Crimp
    Deformation
    Sliding

## Slide 6: Mechanical Response to Load
Quasistatic
  Stiffness
  Modulus
  Max stress, strain
  Toe mod
  Transition stress, strain
Viscoelastic
  Stress relaxation
    Percent relaxation
  Creep
  Dynamic modulus
  Tan delta
Fatigue
  Cycles to failure
  Tangent stiffness
  Peak cyclic strain
  Hysteresis
  Laxity/damage

## Slide 7: Elastic behavior
Load-displacement response

## Slide 8: Elastic behavior
Stress-Strain response

## Slide 9: Experimental Factors Influencing Tendon Properties
Testing environment
  Temperature, humidity
Gripping
  minimize slipping and stress concentrations
Rate of loading
Proper specimen storage
Strain measurement
  Grip-to-grip
  Local: contact, non-contact

## Slide 10: Experimental Factors Influencing Tendon Properties
Initial length
  Small pre-load
Specimen type and orientation
  bone-tendon-muscle complex often tested experimentally
  anatomic orientation, fibers engaged longitudinally
Cross-sectional area
  Contact, non-contact
Specimen geometry
  Whole tendon vs. fiber bundles

## Slide 11: Temperature
Body temp or room temp?
  Be consistent
  But body temp is always recommended

## Slide 12: Humidity
Tendons can dry out pretty fast
  Especially mouse/rat tendons
It is always better to test in a saline bath
  Might not be feasible for large animal tendons

## Slide 13: Specimen storage
Store at -20C
If mouse or rat
  Leaving tendon in body and freezing whole body is best
  If not possible
    Wrap in saline soaked gauze and tightly packed in plastic bag
    Also can do this for larger tendons/tissues

## Slide 14: Gripping
Extremely critical step
  Tendons are very slippery
  Need to remove all muscle from one end
  Can secure bony end in PMMA
  We make custom aluminum grips
    And a combination of sandpaper and superglue
  Essential to do practice samples to check method and that no slippage occurred
  Can mark a line under grip and track if it separates from bottom of grip as load increases

## Slide 15: Strain measurement
Grip-to-grip
  Usually means you calculated strain using the displacement data collected by the testing machine
Local measurements
  Some kind of marker placed/etched/painted/sprayed on the tendon
  Software tracks the texture to calculate displacement
  Removes system compliance artifacts
  Definitely more effort
What kind of markers?
  Verhoeff’s stain
  India ink
  Reflective markers
  Extensometer

## Slide 16: Cross-sectional Area

## Slide 17: What can we test?
Tendons
  Supraspinatus
  Achilles
  Patellar
  Flexor Digitorum Longus
Ligament
  ACL
Skin

## Slide 18: How do we test the supra?
Commonly ruptures with advancing age
Failure usually at the insertion to humeral head

## Slide 19: How do we test the supra?
Humerus in PMMA
Myotendinous junction clamped after sandpaper sandwich
Dots to get local strain

## Slide 20: How do we test Achilles tendon?
Injuries in active and younger people (Kevin Durant…)
Usually fails in the mid-substance
Pay attention to physiological loading direction

## Slide 21: How do we test the Achilles?

## Slide 22: How do we test the patellar tendon?
It is a tendon, but the termini are bony
  We use this to our advantage
A superficial tendon, which makes it a great model to investigate basic science of injury & healing

## Slide 23: How do we test the patellar tendon?

## Slide 24: How do we test the patellar tendon?

## Slide 25: How do we test FDL?
Too long to test all of it
Usually we take a section of it
Both ends are held with sandpaper/glue
This is how we also test skin

## Slide 26: How do we test the FDL?

## Slide 27: How do we test ACL?
It is a ligament
Commonly injured in athletes and younger active women (sorry, Klay Thompson)
  Thus we have two bony ends (femur and tibia)
It is relatively easier to test ligaments

## Slide 28: How do we test the ACL?
We have an AP laxity test setup
  2019 ORS podium in collaboration with Dyment lab

## Slide 29: How do we test the ACL?
How do we get cross sectional area of the ACL?

## Slide 30: How do we test the ACL?

## Slide 31: How do we test the ACL?

## Slide 32: Gauge length Vs. Tendon length
Gauge length
  Measured with the same nominal load applied to all tendons in all groups
Tendon length
  Usually referring to in vivo measurements such as MRI or Ultrasound

## Slide 33: Viscoelastic behavior
Stress Relaxation
  Instantaneous strain application to a constant value
  Observe corresponding change in force

## Slide 34: Viscoelastic behavior
Creep
  Instantaneous force application to a constant value
  Observe corresponding change in strain

## Slide 35: Cyclic Loading
Displacement control cyclic loading at varying frequencies (frequency sweep).
Calculate parameters such as:
  Dynamic modulus
  tan(δ)

## Slide 36: Dynamic Modulus

## Slide 37: Tan(δ)
  - phase lag between stress and strain
    Storage modulus
    Loss modulus

## Slide 38: Fatigue
Load-controlled cyclic loading
  For example: an Achilles tendon undergoes fatigue during activities such as running